Chapter 1

Problem Solutions

1.1

- fcc: 8 corner atoms 18=1atom

6 face atoms  12=3atoms

Total of 4 atoms per unit cell

- bcc: 8 corner atoms 18=1atom

1 enclosed atom        =1 atom

Total of 2 atoms per unit cell

- Diamond: 8 corner atoms 18=1atom

6 face atoms 12=3atoms

4 enclosed atoms   = 4 atoms

Total of 8 atoms per unit cell

_______________________________________

1.2

- Simple cubic lattice:  a=2r

Unit cell vol =a3=2r3=8r3

1 atom per cell, so atom vol =14πr33

Then

Ratio =4πr338r3×100%=52.4%

- Face-centered cubic lattice

d=4r=a2⇒a=d2=22⋅r

Unit cell vol =a3=22⋅r3=162⋅r3

4 atoms per cell, so atom vol =44πr33

Then

Ratio =44πr33162⋅r3×100%=74%

- Body-centered cubic lattice

d=4r=a3⇒a=43⋅r

Unit cell vol =a3=43⋅r3

2 atoms per cell, so atom vol =24πr33

Then

Ratio =24πr334r33×100%=68%

- Diamond lattice

Body diagonal =d=8r=a3⇒a=83⋅r

Unit cell vol =a3=8r33

8 atoms per cell, so atom vol =84πr33

Then

Ratio =84πr338r33×100%=34%

_______________________________________

1.3

- a=5.43Ao; From Problem 1.2d,

a=83⋅r

Then r=a38=5.4338=1.176Ao

Center of one silicon atom to center of

nearest neighbor =2r=2.35Ao

- Number density =85.43×10−83=5×1022cm−3

- Mass density

=ρ=NAt.Wt.NA=5×102228.096.02×1023

⇒ρ=2.33 grams/cm3

_______________________________________

1.4

- 4 Ga atoms per unit cell

Number density =45.65×10−83

⇒Density of Ga atoms =2.22×1022cm−3

4 As atoms per unit cell

⇒Density of As atoms =2.22×1022cm−3

- 8 Ge atoms per unit cell

Number density =85.65×10−83

⇒Density of Ge atoms =4.44×1022cm−3

_______________________________________

1.5

From Figure 1.15

- d=a232=0.4330a

=0.43305.65⇒d=2.447 Ao

- d=a22=0.7071a

=0.70715.65⇒d=3.995 Ao

_______________________________________

1.6

sinθ2=a22a23=23⇒θ2=54.74°

⇒θ=109.5°

_______________________________________

1.7

(a) Simple cubic:  a=2r=3.9 Ao

(b)  fcc:  a=4r2=5.515 Ao

(c) bcc:  a=4r3=4.503 Ao

(d) diamond:  a=24r3=9.007 Ao

_______________________________________

1.8

- 21.0352=21.035+2rB

rB=0.4287 Ao

- a=21.035=2.07 Ao

- A-atoms:  # of atoms =8×18=1

Density =12.07×10−83

=1.13×1023cm−3

B-atoms: # of atoms =6×12=3

Density =32.07×10−83

=3.38×1023 cm−3

_______________________________________

1.9

- a=2r=4.5 Ao

# of atoms =8×18=1

Number density =14.5×10−83

=1.097×1022cm−3

Mass density =ρ=NAt.Wt.NA

=1.0974×102212.56.02×1023

=0.228gm/cm3

- a=4r3=5.196 Ao

# of atoms

Number density =25.196×10−83

=1.4257×1022cm−3

Mass density =ρ=1.4257×102212.56.02×1023

=0.296gm/cm3

_______________________________________

1.10

From Problem 1.2, percent volume of fcc

atoms is 74%;  Therefore after coffee is

ground,

Volume = 0.74 cm3

_______________________________________

1.11

(b)a=1.8+1.0=2.8Ao

- Na:  Density =122.8×10−83

=2.28×1022cm−3

Cl: Density =2.28×1022cm−3

- Na:  At. Wt. = 22.99

Cl:   At. Wt. = 35.45

So, mass per unit cell

=1222.99+1235.456.02×1023=4.85×10−23

Then mass density

ρ=4.85×10−232.8×10−83=2.21 grams/cm3

_______________________________________

1.12

- a3=22.2+21.8=8Ao

Then  a=4.62Ao

Density of A:

=14.62×10−83=1.01×1022cm−3

Density of B:

=14.62×10−83=1.01×1022cm−3

- Same as (a)

- Same material

_______________________________________

1.13

a=22.2+21.83=4.619 Ao

(a)  For 1.12(a), A-atoms

Surface density =1a2=14.619×10−82

=4.687×1014cm−2

For 1.12(b), B-atoms:   a=4.619 Ao

Surface density =1a2=4.687×1014cm−2

For 1.12(a) and (b), Same material

(b)  For 1.12(a), A-atoms; a=4.619 Ao

Surface density

=1a22=3.315×1014cm−2

B-atoms;

Surface density

=1a22=3.315×1014cm−2

For 1.12(b), A-atoms; a=4.619 Ao

Surface density

=1a22=3.315×1014cm−2

B-atoms;

Surface density

=1a22=3.315×1014cm−2

For 1.12(a) and (b), Same material

_______________________________________

1.14

- Vol. Density =1ao3

Surface Density =1ao22

- Same as (a)

_______________________________________

1.15

- (110) plane

(see Figure 1.10(b))

(ii) (111) plane

(see Figure 1.10(c))

(iii) (220) plane ⇒12, 12, ∞⇒1, 1, 0

Same as (110) plane and [110] direction

(iv) (321) plane ⇒13, 12, 11⇒2, 3, 6

Intercepts of plane at

p=2, q=3, s=6

[321] direction is perpendicular to

(321) plane

_______________________________________

1.16

(a)

11,13,11⇒313

(b)

14,12,14⇒121

_______________________________________

1.17

Intercepts: 2, 4, 3  ⇒12, 14, 13⇒

(634) plane

_______________________________________

1.18

- d=a=5.28Ao

- d=a22=3.734 Ao

- d=a33=3.048 Ao

_______________________________________

1.19

- (a) Simple cubic

(i) (100) plane:

Surface density =1a2=14.73×10−82

=4.47×1014cm−2

(ii) (110) plane:

Surface density =1a22

=3.16×1014cm−2

(iii) (111) plane:

Area of plane =12bh

where b=a2=6.689 Ao

Now

h2=a22−a222=34a22

So  h=624.73=5.793 Ao

Area of plane

=126.68923×10−85.79304×10−8

=19.3755×10−16cm2

Surface density =3×1619.3755×10−16

=2.58×1014cm−2

(b) bcc

(i) (100) plane:

Surface density =1a2=4.47×1014cm−2

(ii) (110) plane:

Surface density =2a22

=6.32×1014cm−2

(iii) (111) plane:

Surface density =3×1619.3755×10−16

=2.58×1014cm−2

(c) fcc

(i) (100) plane:

Surface density =2a2=8.94×1014cm−2

(ii) (110) plane:

Surface density =2a22

=6.32×1014cm−2

(iii) (111) plane:

Surface density =3×16+3×1219.3755×10−16

=1.03×1015cm−2

_______________________________________

1.20

- (100) plane: - similar to a fcc:

Surface density =25.43×10−82

=6.78×1014cm−2

- (110) plane:

Surface density =425.43×10−82

=9.59×1014cm−2

- (111) plane:

Surface density =23/25.43×10−82

=7.83×1014cm−2

_______________________________________

1.21

a=4r2=42.372=6.703 Ao

- #/cm3=8×18+6×12a3=46.703×10−83

=1.328×1022cm−3

- #/cm2=4×14+2×12a22

=26.703×10−822

=3.148×1014cm−2

- d=a22=6.70322=4.74 Ao

- # of atoms =3×16+3×12=2

Area of plane:  (see Problem 1.19)

b=a2=9.4786 Ao

h=6a2=8.2099 Ao

Area =12bh=129.4786×10−88.2099×10−8

=3.8909×10−15cm2

#/cm2=23.8909×10−15

=5.14×1014 cm−2

d=a33=6.70333=3.87 Ao

_______________________________________

1.22

Density of silicon atoms =5×1022cm−3 and

4 valence electrons per atom, so

Density of valence electrons =2×1023cm−3

_______________________________________

1.23

Density of GaAs atoms

=85.65×10−83=4.44×1022cm−3

An average of 4 valence electrons per atom,

So

Density of valence electrons

=1.77×1023cm−3

_______________________________________

1.24

- 5×10175×1022×100%=10−3%

- 2×10155×1022×100%=4×10−6%

_______________________________________

1.25

- Fraction by weight

2×101610.825×102228.06=1.542×10−7

- Fraction by weight

101830.985×102228.06=2.208×10−5

_______________________________________

1.26

Volume density =1d3=2×1016cm−3

So  d=3.684×10−6cm

We have  ao=5.43 Ao

Then  dao=368.45.43=67.85

_______________________________________

1.27

Volume density =1d3=4×1015cm−3

So  d=6.30×10−6cm ⇒d=630 Ao

We have ao=5.43 Ao

Then  dao=6305.43=116

_______________________________________